Nanopatterning of silicon surfaces by ultrashort laser pulses

A.A. Nastulyavichus1, S.I.Kudryashov1,2, I.N. Saraeva1, A.A. Rudenko1,A. A. Ionin1 , D.A. Kirilenko3,A.L. Shakhmin4 and E.R. Tolordava1,5.

1 Lebedev Physical Institute, Moscow, Russia

2 ITMO university, St. Petersburg, Russia

3 Ioffe Institute, St.-Petersburg, Russia

4Peter the Great Politechnic University, St.-Petersburg, Russia

5N.F. Gamaleya Federal Research Centre of Epidemiology and Microbiology, Moscow, Russia

e-mail: ganuary_moon@mail.ru

Fabrication of ultrafine surface nanoripples by ultrashort (0.1-10 ps) laser pulses has proved for a long time to be a “green”, fast technology for large-scale surface nanopatterning in the form of regular arrays of surface 1D-nanowires or 0 D-nanodots, broadly used for nanophotonic and biomedical  applications [1-2].

Large-scale surface nanopatterning of silicon wafer covered by a 5-mm thick liquid carbon disulfide layer, in the form of regular 1D-arrays of vertical nanosheets was performed by multiple focused 0.3- and 10-picosecond infrared (IR) laser pulses via excitation of deep sub-wavelength plasmons on the photoexcited silicon surface. Sub-micron thick silicon surface layers demonstrate the exposure-tunable near-IR– mid-IR optical density and related sulfur, carbon and oxygen contents. Transmission electron microscopy, electron diffraction and micro-Raman spectroscopy reveals the amorphous structure of the sulfur-hyperdoped nanosheets atop their slightly distorted crystalline basements. Their crystallographic structure and elemental distributions indicate their exposure-dependent growth via deposition of silicon and sulfur species from the interfacial vapor/plume bubbles, provided by Si ablative nanoplumes from the regular ablative trenches and carbon disulfide decomposition in the plumes/bubbles.

The fabricated nanocoatings demonstrate the remarkable anti-bacterial modality relative to Gram-positive bacteria (Staphylococcus aureus) [3].

The reported study was funded by RFBR according to the research project № 18-29-20022

REFERENCES

[1] E.V. Golosov, A.A. Ionin, Yu. R. Kolobov, S. I. Kudryashov, A.E. Ligachev, S. V. Makarov, Yu. N. Novoselov, L.V. Seleznev, D.V. Sinitsyn,   Appl. Phys. A. 104, 701-705 (2011).

[2] A.A. Ionin, S.I. Kudryashov, S.V. Makarov, L.V. Seleznev, D.V. Sinitsyn, Laser Phys. Lett. 12, 025902 (2015).

[3] S.I. Kudryashov, L.V. Nguyen, D.A. Kirilenko, P.N. Brunkov, A.A. Rudenko, N.I. Busleev, A.L. Shakhmin, A.V. Semencha, R.A. Khmelnitsky, N.N. Melnik, I.N. Saraeva, A.A. Nastulyavichus, A.A. Ionin, E.R. Tolordava, and Y.M. Romanova, ACS Applied Nano Materials. 1(6), 2461-2468 (2018).