Fluorescent proteins as perspective elements of optoelectronic devices

A.S. Kudriavtseva1,2, N.P. Nekrasov3, I. Bobrinetskiy2,4

1Prokhorov General Physics Institute of the Russian Academy of Sciences, Moscow, Russia

2Moscow Institute of Physics and Technology, Moscow Region, Russia

3National Research University of Electronic Technology, Moscow, Russia

4*BioSense Institute - Research and Development Institute for Information Technologies in Biosystems, University of Novi Sad, Novi Sad, Serbia

e-mail: bobrinet@gmail.com

Fluorescent proteins (FPs) are widely used in biomolecular research due to their high quantum yield and stability. A broad range of engineered FPs have been developed, enabling tuning their spectral sensitivity, wavelength conversion, and chemical modifications. Recently, FPs were proposed as a light converter for photovoltaics and bioelectronics applications.

In this work, we demonstrate the functionalization of field-effect transistors based on individual single-walled carbon nanotubes (SWCNT-FETs) with FPs to introduce novel optoelectronic properties (Figure 1a). We employed a developed protein immobilization approach on carbon nanomaterials, that have been used also for biosensor development [1].

First, the sensitivity of green FPs (GFPs) photochemically immobilized on carbon lattices was investigated and specific photoresponse at 470 nm (Figure 1b) was shown [2]. Two types of engineered proteins have been studied with different positions of introduced non-natural amino acids containing phenyl-azide chemistry: the barrel wall of GFP and the bottom side. We demonstrated that the photoresponse is site-specific, and influenced by the number of charge traps associated with the hydrophobicity of the protein surface (Figure 1c).

Additionally, for SWCNT-FETs functionalized with red FPs, we used a PBASE linker adsorbed onto the nanotube surface [3]. These devices exhibit an unexpected gating effect on channel conductivity under FP-specific light irradiation. In this configuration, electrons can only transfer from the FPs when the gate voltage is below the threshold voltage, resulting in a negative photoresponse.

Thus, engineering of FPs pave a way for novel optoelectronic devices with tunable properties.

Figure 1. The performance of FP/SWCNT FET. (a) Scheme of SWCNT-FET with immobilized fluorescent proteins. (b) Spectral selectivity of bio-FET response. (c) The role of FPs immobilization site with memory response (top) and photodetector mechanism (bottom).

REFERENCES

[1] N. Nekrasov, S. Jaric, D. Kireev, et al. Biosens. Bioel. 200, 113890 (2022).

[2] A.S. Kudriavtseva, N.P. Nekrasov, D.V. Krasnikov, et al., Adv. Electron. Mater. 11, 2400329 (2025).

[3] R.E. Gwyther, N.P. Nekrasov, A.V. Emelianov, et al., Adv. Funct. Mater. 32, 2112374 (2022).