Measuring electronic properties of free-standing nanocrystals for solar cell absorbers

A. R. Milosavljević1*, D. K. Božanić2, D. Danilović2, P. Sapkota3,4, N. Vukmirović5, S. Sadhu3, 
R. Dojčilović2, W. Huang3,4,6,  J. Bozek1, C. Nicolas1, L. Nahon1, and S. Ptasinska3,4

1Synchrotron SOLEIL, l’Orme des Merisiers, Saint Aubin, BP48, 91192 Gif sur Yvette Cedex, France

2Vinca Institute of Nuclear Sciences, University of Belgrade, P.O. Box 522, 11001 Belgrade, Serbia

3Radiation Laboratory, University of Notre Dame, Notre Dame, Indiana 46556, United States

4Department of Physics, University of Notre Dame, Notre Dame, Indiana 46556, United States

5Institute of Physics Belgrade, University of Belgrade, Pregrevica 118, 11080 Belgrade, Serbia

6Department of Chemical Engineering, Stanford University, Stanford, California 94304, United States

e-mail: milosavljevic@synchrotron-soleil.fr

We will describe a novel experimental technique that combines surface XPS and gas-phase synchrotron radiation-based XPS/VUV PES, for the investigation of the electronic structure of different nanocrystals that could be low-cost and high-efficient solar cell absorbers [1]. Surface XPS is performed in Notre Dame University (US) using SPECS Surface Nano Analysis GmbH, with a PHOIBOS 150 hemispherical energy analyzer. The synchrotron based XPS/PES is performed at the SOLEIL synchrotron (France). For gas-phase PES, the nanoparticle beam is produced by an atomizer and focused by the aerodynamic lens into the interaction region. On DESIRS beamline, the angle-resolved photoemission spectra were measured by double imaging DELICIOUS3 spectrometer (VMI for electrons and VMI-TOF for ions). On PLEIADES, the ±30o aperture wide-angle lens VG-Scienta R4000 electron analyzer was used to record the XPS. The nanoparticles are synthetized both at Vinca Institute of Nuclear Sciences (Serbia) and in Notre Dame. The experimental results are supported by DFT calculations performed at the Institute of Physics Belgrade (Serbia).

Recent results for lead halide perovskites [1] will be presented, as well as preliminary results for lead-free materials such as Ag-Bi-I rudorffite nanosystems. The procedure to synthetize nanoparticles of this material for aerosol generation has been most recently developed at Vinca Institute of Nuclear Sciences. We were able to obtain a complete band alignment to the vacuum of the nanocrystals and investigate their surface properties with high sensitivity.

REFERENCES

[1] Milosavljević A. et al, J. Phys. Chem. Letters 9 3604 (2018)