Non-Linear Excitation Fluorescence Imaging through

Two-Photon Laser Polymerized Microlenses

G. Chirico1, M. Marini1, R. Martínez Vázquez2, R.Osellame2, A. Nardini3, C. Conci3, E. Jacchetti3, D. Panzeri1, L. Sironi1, M. Bouzin1, M. Collini1, D. Inverso4, B.S. Kariman5, E. Kabouraki6, M. Farsari6, , G. Cerullo5 and M.T. Raimondi3

1 Dept. of Physics, Università di Milano-Bicocca, Milan, Italy

2 Institute for Photonics and Nanotechnologies (IFN)-, CNR Politecnico di Milano, Milan, Italy

3 Dept. of Chemistry,Materials and Chemical Engineering “Giulio Natta”, Politecnico di Milano, Milan, Italy

4 Div. of Immunology, IRCCS San Raffaele Scientific Institute, Vita-Salute San Raffaele University, Milan, Italy.

5 Dept. of Physics, Politecnico di Milano, Milan, Italy

6 Forth- Institute for Electronic Structure and Lasers, Heraklion, Crete, Greece

e-mail:Giuseppe.chirico@unimib.it

# We report on methods for laser fabrication of microlenses by 2 Photon Polymerization (2PP) and their use for non-linear excitation microscopy. These lenses can help, once implanted, to reduce the spherical aberrations induced by the tissue in in vivo imaging.

Microlenses have already been fabricated by 2PP [1] but with too low numerical aperture to allow non-linear excitation microscopy. Therefore, up to now, no attempt has been made to use laser fabricated microlenses for non-linear excitation fluorescence microscopy of biological samples.

We show that microlenses with high numerical aperture (0.4) and large diameter (280μm), can be fabricated with a medium throughput, about 8 minutes/lens, by limiting the 2PP fabrication to a ≃ 5 μm thick outer crust, followed by a post-development volume polymerization. This procedure leads to sufficient optical quality (roughness ≃ 80nm) to use the lenses for fluorescence confocal and two-photon excitation microscopy. We report on the use of the microlenses for fluorescence non-linear excitation microscopy of cells cultures (Figure 1) and thick specimens [2].

Figure 1. A: Confocal image of human fibroblasts (FITC-phallodin, cytoskeleton and DRAQ5/Hoechst, nuclei staining). B: fluorescence confocal image through a microlenses array. C: Cropped scan area through a single microlens. D: Full field-of-view confocal microscope image of cells at the glass coverslip focal plane (20x dry objective for A-D). E: 3D reconstruction of cells through an array of microlenses. F-I: Fluorescence images of the cells under two-photon excitation (λ=800 nm). F: Fluorescence image through the microlenses coupled to a 20x dry objective. G: Control image through the 20x dry objective. H: Image of the cells through the microlenses coupled to a 25x water immersion objective. I: Control image through the 25x water immersion objective.

This work opens the possibility to use implanted micro-lenses for non-linear excitation of tissues, allowing the direct and continuous optical inspection of biological dynamics in vivo.

REFERENCES

[1] D. Gonzalez-Hernandez, B. Sanchez-Padilla, D. Gaileviˇcius, et al. Adv. Optical Mater., 2300258, 2023.

[5] M. Marini, A. Nardini, R. Martínez Vázquez et al. Adv. Fun. Mater. 2213926, 2023.

Acknowledgments. This project has received funding from the EU Horizon 2020 programme (G.A. No 964481).